## Slide 1: Process Simulation of Directed Energy Deposition process using COMSOL Multiphysics®
Vaibhav Naina,*
a Irepa Laser, Parc d’Innovation, 67400 Illkirch-Graffenstaden, France

## Slide 2: Thermo-mechanical Simulation for DED
DED
Why simulation?
Challenge!
Project Goals!

## Slide 3: Directed Energy Deposition (DED)
Material | Ti-6Al-4V
Construction | Total : 33h
Weight | 14,2kg
Length | 1070 mm
Part defects
Distortion accumulation > 20 mm
Part rejected
DED fabricated part failure
Digital test
What if!
Material | Ti-6Al-4V
Construction | Total : 155h
Weight | 71kg
Diameter | 680 mm

## Slide 4: Why simulation?
Simulate DED process
Predict part response
Distortion-compensated CAD
Trial & error approach
Lots of time & money
Cannot predict deformation
Digital Chain: Currently used in industry for large-part fabrication
Ideal: Complete the missing link
4
4
PROCESS PARAMETERS
OPTIMIZATION
Specify additive material
Apply deposition strategies
Finish & obtain deposition path
5
3
2
1
CAD DESIGN
& OPERATIONS
CAM
PROGRAMMING
MACHINE
SIMULATION
PROCESS PARAMETERS
OPTIMIZATION
PART
FABRICATION
Transfer CAM to DED machine
Part fabrication
Process data optimization
Machine simulation
Collisions verification
Machine & path verification
Perform & finalize part design
Decompose part geometry
Different operations on bodies

## Slide 5: Challenge!
Computation time
Meso-scale
Part-scale
Flash Heating (FH)
Sequential FH (SFH)
Inherent Strain
Simulates laser movement
Simulates melt-pool scale
Do not simulate laser movement
Simulates layer scale
Meso: Calculate Inherent Strain
Part: Apply Inherent Strain
Simulates laser movement
Simulates sub-layer scale
Model | Computation speed | Computation accuracy | Large-part simulation
Meso scale |  |  | 
FH |  | ? | 
SFH |  |  | 
Inherent-strain |  |  | 
Model | Computation speed | Computation accuracy | Large-part simulation
Meso scale |  |  | 
FH |  | ? | 
SFH |  |  | 
Inherent-strain |  |  | 
AS OF TODAY: THE MODELING STRATEGY FOR LARGE DED PART IS NOT VALIDATED
COMPUTATION TIME & ACCURACY
[1]
[2]
[3]
[4]
V. Nain (PhD 2019-22)

## Slide 6: Project Goals!
Digital tool for large-part DED
5
4
3
2
1
INVESTIGATE: Current modeling methods
DEVELOP: DED process simulation model
FOCUS: Computation time reduction
VALIDATE: With experiment data
OUTCOME: PREDICTIVE SIMULATION TOOL FOR LARGE-PART DED

## Slide 7: Methods and use of COMSOL Multiphysics®
Experiment
Numerical model development
Numerical model set-up
Numerical analyses

## Slide 8: Experiment
Experiment DOE
MATERIAL
Substrate: S235
Build part: SS 316L
LASER
: 800 W
: 1 m/min
: 2.2 mm
DIMENSIONS
100 layers (2 tracks/layer)
Total weld length: 80 m
6.97 mm
Scan data v/s CAD
Experiment
CAD
Sensors location

## Slide 9: Numerical model development
FH & Layer Lumping method for DED
SUBSTRATE
Currently heated for th
Undeposited (quiet)
Undeposited (quiet)
SUBSTRATE
Currently cooled for tcool
Undeposited (quiet)
Undeposited (quiet)
SUBSTRATE
Previously deposited
Currently heated for th
Undeposited (quiet)
(a) Time decomposition for a single layer (b) FH method schematic
(a)
(b)
No lumping
∆zt: 0.45 mm
2-layer lumping
∆zt: 0.9 mm
4-layer lumping
∆zt: 1.8 mm
8-layer lumping
∆zt: 3.6 mm
Layer lumping method
Sim. parameters | Lumping configuration |  |  | 
 | No | 2 | 4 | 8
Macro layers | 100 | 50 | 20 | 10
∆zt (mm) | 0.45 | 0.9 | 1.8 | 3.6
Mesh elements | 58970 | 37136 | 32203 | 28305

## Slide 10: Numerical model set-up
Thermal expansion (te)
Coupling link between ht & sm
Multi-physics
Multiphysics simulation
Laser heat input
Heat losses (convective & radiative)
Elasto-plastic model
Non-linear material hardening (Voce)
Discrete states i.e., FH (1 or 0)
Explicit Events (theat & tcool)
Heat transfer in solids (ht)
Solid mechanics (sm)
Events (ev)
Material activation: Quiet element (sm)
Material properties f(T)
Material

## Slide 11: Numerical analyses
Thermal
Simulation
Sequential coupling
Mechanical Simulation
Thermal strain
Thermal strain
Temperature
field
Deformation
Stresses
Process parameters
CAD (sliced layers)

## Slide 12: EXP v/s SIM
Simulation results

## Slide 13: Simulation results
EXP v/s SIM (Thermal)
No lumping
2-layer
4-layer
8-layer

## Slide 14: Simulation results
EXP v/s SIM (Mechanical)
Final z-distortion (mm) | LDS location
Experimental | 3.88
No-lumping simulation | 4.83
2-layer lumping simulation | 3.65
5-layer lumping simulation | 2.89
10-layer lumping simulation | 1.53
No lumping
2-layer
4-layer
8-layer

## Slide 15: Simulation results
EXP v/s SIM (Mechanical)
6.97 mm
EXPERIMENT
2.09 mm
3.98 mm
5.06 mm
6.68 mm
No lumping
2-layer lumping
8-layer lumping
4-layer lumping

## Slide 16: Project Impact!
Industrial part simulation

## Slide 17: Industrial part simulation
“ PRINT PART 1st TIME RIGHT ”
CAM
0s
60s
MECHANICAL
SIMULATION
THERMAL SIMULATION
CAD
Size 128 x 660 mm
Fabricated part with 60s cooling
EXP: DEFORMATION
Influence of inter-layer dwell time (SIM)
With an addition of 60s in simulation (optimized value)
  Peak temperatures are controlled during fabrication.
  Deformation is reduced by 43%. Validated with EXP data.
  Complex part “ PRINTED 1st TIME RIGHT “.
Helical rotor of a Moineau™ cavity pump
Computation time:
Thermal analysis: 65 min
Mechanical analysis: 32 min

## Slide 18: Conclusions
03
02
01
06
05
04
FH method with energy conservation rule is accurate
Layer lumping drastically reduces the computation time
Layer lumping negatively affects computation accuracy
Layer lumping size needs to be calibrated
Suitable for large-part simulation
Further validation on industrial part is required
Conclusions

## Slide 19: Contact-us !
Vaibhav Nain
vn@irepa-laser.com