## Slide 1: Advanced multi-physics models for the optimization of the hot extrusion process of light alloys
R. Pelaccia1*, B. Reggiani1, M. Negozio2, S. Di Donato3, L. Donati3
DISMI - Department of Sciences & Methods for Engineering. University of Modena & Reggio Emilia
DISTI– Department of Engineering for Industrial Systems and Technologies University of Parma
DIN- Department of Industrial Engineering, University of Bologna
*Corresponding author email: riccardo_p@unimore.it

## Slide 2: The hot extrusion process of light alloys
Some Fields of Application:
Furniture design
Automotive
Aeronautics
Railway transportation
Construction…
Extruded Aluminum:
High geometric complexity
High strength-to-density ratio
High Corrosion Resistance
High Crash Resistance…
High quality and shape complexity required
Very competitive market
Show the recent advancements in the simulation of the extrusion process
The use of simulation becomes essential
Aim of the work

## Slide 3: From real process to numerical simulation
Deformation energy and friction forces are converted into heat
High temperatures are necessary to promote the proper material flow and to reduce the extrusion load
Exit profile temperature can limit the maximum productivity (nitrogen cooling possible solution)
Continuous process (high productivity) lead to interaction between two subsequent billet (unavoidable defects)
Prediction of thermal field and extrusion load
Prediction of material flow behavior
Tooling-set stress analysis
Prediction of extrusion defects
Involved phenomena
Identify what is necessary to simulate

## Slide 4: Model Implementation (Uncooled Extrusion Process)
Container and Ram replaced with equivalent thermal and frictional conditions (Eulerian approach )
Material under deformation treated as a fluid at very high viscosity (Laminar Flow)
Viscosity is temperature and strain-rate depended (Zener-Hollomon model)
Heat Transfer and Laminar Flow equations are coupled
Solid Mechanics Interface is added for the tooling set stress analysis
Real Extrusion Process
COMSOL Model

## Slide 5: Model Implementation (Extrusion Process with Nitrogen Cooling)
The 3D model of extrusion process is coupled with 1D model of cooling channel
Non-Isothermal Pipe Flow is added and coupled with the Heat Transfer interface
If necessary, a preliminary evaluation of the channel design is possible with Topological Optimization interface (Density Model + Porous Media)
Backer is “virtually milled” to obtain the cooling path

## Slide 6: Model Implementation (Extrusion defects)
Since the extrusion is performed in continuous process, a certain length of the profile is contaminated by the interaction between the old and the new billet material for each run.
This contaminated length is unavoidable scrap (low mechanical properties)
Phase field interface was chosen to describe the interaction between two immiscible fluids

## Slide 7: Equations (Material Flow and Heat Exchange)
Navier-Stokes Equations for incompressible flow (Laminar Flow Interface)
Conservation of momentum
Conservation of mass
Viscous term
Perzyna viscoplastic model
Zener-Hollomon Model of material flow stress
Fourier Equations for heat transfer in solid and fluid (Heat Transfer in Solid and Fluid Interface)
COUPLED SYSTEM

## Slide 8: Equations (Die-stress analysis)
Fixed
Fixed
Aluminum under deformation
Tooling set subjected to compression state
Solid Mechanics Interface
Momentum balance
Pressure on die-set from Laminar Flow Interface
Thermal expansion from Heat Transfer Interface

## Slide 9: Equations (Nitrogen Cooling)
Conservation of the momentum
Conservation of the mass
Heat transfer equation
4. Convective contribute with the die
5. Heat transfer equation for the die
-
h is not constant
Density Approach
output material volume factor
0 solid
1 liquid
Penalization functions
Permeability
Conductivity
Density
Specific Heat Capacity
Non-Isothermal Pipe Flow Interface
Hydraulic diameter variable along the path
Heat Transfer in Solid and Fluid interface
Phase change of nitrogen is not simulated
Cp, r, k function of temperature to consider the effect of nitrogen phase change (Homogenous fluid model)
Topological Optimization interface
Porous domain virtually milled

## Slide 10: Equations (Extrusion defects)
Chemical Potential
Surface tension
Mobility tuning parameter
ϕ phase field parameter:
-Value 0 fluid 1
-Value 1 fluid 2
Velocity field from Laminar Flow interface
Cahn-Hilliard equation

## Slide 11
Case Study 1: Multi-die design with conformal cooling channel
Insert for extrusion die realized with 3D manufacturing technology (SLM)
Helicoidally conformal cooling channel
COMSOL Model and Process Parameters
Thermocouple hole
RESULTS
Thermal History recorded by the thermocouple
Die stress analysis
Insert resisted the whole campaign without defects
All points under the yield stress

## Slide 12
Case Study 2: Phase field method for the assessment of the new-old billet material interaction
New billet material (visible after chemical etching)
Excessive scrap
or
Not Enough Scrap
Experimental Analysis is a time and cost consuming activity
Empirical and analytical approach not accurate
Distance from the stopmark

## Slide 13
Case Study 3: Cooling Channel re-design by means of topological optimization interface
Channel designed by the die maker without numerical tools
Experimental results evidenced not efficient cooling
Numerical error below 10%
Same inlet of original design, outlets reduced from 16 to 10
Temperature control points for objective function (balanced cooling around the die exit)
Maximum 25% of hollowed-out volume for cooling channel as constraint
Velocity field of nitrogen
Topological optimization
Same process parameters of the experimental trial
Gas formation
Gas formation

## Slide 14
Case Study 4: Multi-objective optimization of extrusion die
Parametric CAD
COMSOL with Matlab
Optimization Platform
(Modefrontier)
Initial Population
Test automatically all initial configuration
Objective Functions
Constraints
Genetic Algorithm to optimize the problem
Change variable
Define new design
Test the new design
In the original die design a break occurred after 64 extrusion.
The optimal design showed a peak principal die stress reduced of 46%
Ram speed doubled
Mechanical properties of profile improved
Balanced cooling with the optimized design (max temperature difference from 60°C to 16°C)
Nitrogen consumption reduced of 60%
MULTI-OBJECTIVE OPTIMIZATION OF COOLING CHANNEL

## Slide 15: Conclusions
Different interfaces were coupled to generate advanced models able to assess the hot extrusion process from different points of view.
The accuracy of numerical predictions was demonstrated in terms of extrusion load, thermal field, scrap assessment, cooling efficiency, and die stress analysis.
The experimental-numerical comparisons also showed the limits of industrial practices, sometimes based on experience and/or empirical approaches.
An advanced iterative procedures based on the use of genetic algorithms evidenced the concrete possibility of automatically optimizing the die design as well as the entire process concerning the objectives to be achieved.
References
R. Pelaccia, M. Negozio, et al., “Extrusion of Light and Ultralight Alloys with Liquid Nitrogen Conformal Cooled Dies: Process Analysis and Simulation”, J. Mater. Eng. Perform. 31, pp. 1991-2001, 2021.
S. Di Donato, R. Pelaccia and M. Negozio, “Phase Field Method for the Assessment of the New-Old Billet Material Interaction during Continuous Extrusion Using COMSOL Multiphysics”, J. of Materi Eng and Perform, 2024.
R. Pelaccia, B. Reggiani, et al., “Investigation on the topological optimization of cooling channels for extrusion dies”, Mater. Res. Proc. 28, pp. 533-542, 2023.
B. Reggiani, L. Donati and L. Tomesani, "Multi-goal optimization of industrial extrusion dies by means of meta-models", Int J Adv Manuf Technol 88, pp. 3281–3293, 2017.
R. Pelaccia, M. Negozio, et al., "Assessment of the Optimization Strategy for Nitrogen Cooling Channel Design in Extrusion Dies", Key Eng Mater. 926, pp. 460–47, 2022.

## Slide 16: THANK YOU FOR YOUR ATTENTION
Contacts:
Riccardo Pelaccia: riccardo_p@unimore.it
Barbara Reggiani: barbara.reggiani@unimore.it
Marco Negozio: marco.negozio@unipr.it
Sara Di Donato: sara.didonato2@unibo.it
Lorenzo Donati: l.donati@unibo.it