## Slide 1
Impact of The Key Aging Mechanisms in NMC-622 Batteries and their Consequences in Degradation
Rifat Rashid Ahmed, Joris de Hoog, Maitane Berecibar & Md. Sazzad Hosen
Electromobility Research Centre-MOBI, Vrije Universiteit Brussel (VUB)- Belgium

## Slide 2: Motivation
Need for upscaling and model optimization for enhancing performance in real life applications with physics-based understanding
Need for fundamental understanding of aging mechanisms to improve battery performance and lifespan
Challenges in understanding and predicting battery aging and safety
Growing demand for reliable battery systems for numerous applications

## Slide 3: What makes battery age?
Electrolyte decomposition
Particle cracking
Lithium-plating
Growth of parasitic SEI layer
Identifying the influences of key aging mechanisms
Need for upscaling and model optimization for enhancing performance in real life applications

## Slide 4
Investigate the impact of these aging mechanisms on battery performance and lifetime
3
Considering other factors- graphite expansion, particle cracking, electrolyte decomposition
2
Coupled degradation mechanisms (SEI and lithium-plating/stripping) applied into electrochemical model
1
Objectives
*Oxford University

## Slide 5: Electrochemical model with aging mechanisms
* Yang et al., Journal of Power Sources, 2017
Desired electrochemical reaction:
  Intercalation of lithium in graphite
Undesired side reactions:
  SEI layer growth
  Lithium-plating
  , E <0 V vs Li

## Slide 6: Electrochemical model with aging: equations
Li-ion intercalation/deintercalation reaction:
P2D electrochemical model
SEI growth current density:
* Ekström et al. 2015
Li-plating/stripping reaction:
if , else
*COMSOL Application Library

## Slide 7: COMSOL Implementation
Degradation Model Tree
Battery design module- LIB
Degradation: SEI and Li-P/Str
Coupling SEI and Li-P
NMC-622/Gr Cylindrical & pouch cells
Degradation- focused on negative electrode
Coupled degradation implemented
SEI: Mixed kinetics and diffusion, graphite expansion, SEI cracking
Li-P/stripping: Reversible reaction, irreversible LLI- dead lithium.
Intercalation

## Slide 8: Parameter Extraction
1. | 2. | 3. | 4.
Physical characterization- SEM, cross-section analysis, radius, porosity, thickness
Test- EIS, HPPC, reference performance test
Few parameters assumed/taken from literature
EIS Test
10um
SEM: Surface Morphology
50um
SEM: Cross-section
Half cell OCV

## Slide 9: Comparison of simulation and experiment
Condition: 1C/0.3C
Cells  EoL
Difference between simulation and experimental discharge curves, RMSE~0.025
Relative capacity from experiments
Increased capacity due to anode overhang effect
Lithium plating observed for 1C/1C cycling after ~250 FEC
Notes:   Simulation follows experimental mean trajectory
  Further aging parameters needed

## Slide 10: Differential Voltage & Incremental Capacity Analysis
1. | 2.
 | 3.
dQ/dV
*Using peak tracking method from J.Chen et al. Journal of Energy Storage 2022
 | % Loss | Capacity fade contribution
,de-Li | 1.1 | 0.7
,Li | 0.1 | 0.1
,Li | 6.7 | 6.6
 | % Loss | Capacity fade contribution
 | 1.1 | 0.7
 | 0.1 | 0.1
 | 6.7 | 6.6
Optimization outputs | 
Calc. capacity fade | 7.48%
Actual capacity fade | 6.35%
Error | 1.13%

## Slide 11: Coupling effect of SEI and Lithium-Plating
SEI layer thickness increases resistance
Film thickness causes potential drop over SEI layer
Drop is more prominent near separator region
SEI growth causes reduction in anode porosity
Leads to lower lithium deposition potential
Triggers the onset of lithium plating
Thus, causing more cell degradation

## Slide 12: Conclusions & Future Scope
SEI and lithium plating degradation mechanisms investigated through electrochemical model
Coupled interaction affects overall cell performance of LIB
SEI layer growth can trigger onset of lithium plating causing non-linear degradation
Future studies will include
  Validation with SEI, lithium plating related parameters
  Upscaling model to module and pack-level

## Slide 13: Acknowledgements
EU funding from HORIZON EUROPE project THOR- Grant agreement number 101103708
Project partners
Prof. Dr. Maitane Berecibar
Professor ,
Vrije Universiteit Brussel
(Planning & supervision)
Dr. Joris de Hoog
Senior Researcher,
Vriije Universiteit Brussel
(Review & editing)
Prof. Dr. MD Sazzad Hosen
Professor,
Vriije Universiteit Brussel (Planning, review & supervision)
The author would like to acknowledge the effort of the following:

## Slide 14
Rashid Ahmed Rifat
PhD Researcher, Battery Innovation Centre, MOBI, Vrije Universiteit Brussel- Belgium
Contact: Email : rashid.ahmed.rifat@vub.be Cell No. : +32472322527
Thank you for your attention
Let’s get connected!