## Slide 1: Electromagnetic Sensing System for Ore Waste Classification and Grade Detection in LHD Buckets
Robert J. Exposito M.¹
1. Mining and rock engineering division, department of civil, environmental and natural resources engineering, Luleå University of Technology, Luleå, Sweden
☎ 0920-493212
✉ robert.exposito@ltu.se
📍 Luleå, T3366

## Slide 2: Agenda
Introduction
    Case study
    Motivation
    Concept overview
    Objectives
Methods
    Simulation setup
    Ore domain preparation
Results
    Homogeneous domain
    Heterogeneous domain
Concluding remarks

## Slide 3: Kiirunavaara mine (Kiruna, Sweden)

## Slide 4: Motivation
Why Improve Ore-Grade Monitoring in Loading Operations?
Current LHD system uses density-based monitoring.
Performance affected by fragmentation, loading volume variation, and moisture.
Need for a continuous reliable approach to corroborate current monitoring data and avoid false positives.

## Slide 5: Concept Overview
Magnetic-Based Monitoring Concept
Uses magnetic field interaction with ore to detect relative permeability contrasts.
Measures mutual inductance (M) between excitation and sensing coils.
𝑀 with 𝜇𝑟​ → ore grade.

## Slide 6: Objectives
Evaluate feasibility of magnetic-based sensing for ore–waste differentiation and grade estimation.
Simulate electromagnetic response under homogeneous and heterogeneous domains.
Assess effect of rock heterogeneity in grade estimation.

## Slide 7: Simulation Setup
COMSOL Model
AC/DC Module
Magnetic fields (mf) + Electrical circuit (cir) interfaces
2D magneto-quasi-static model
DC excitation ramp; steady-state window
Initial condition: 𝑡 = 0 ⇒𝐴 = 0
Output variables: (𝑡) & 𝑀(𝑡)
Domain: ore region (homogeneous and heterogeneous 𝜇𝑟(𝑥,𝑦)
Meshing: particular across ore domain

## Slide 8: Ore Domain
Permeability Distribution in Ore Domain
Example 1 of a heterogeneous relative magnetic permeability field for .
Example 2 of a heterogeneous relative magnetic permeability field for .
Parameter | Level
[mm] | 1, 2, 5, 10, 20
 | 0, 0.5, 1, 2, 5
[H/m] | 2, 4, 6, 8, 10, 12, 14, 16
Parameter | Level
 | 1, 2, 5, 10, 20
 | 0, 0.5, 1, 2, 5
 | 2, 4, 6, 8, 10, 12, 14, 16

## Slide 9: Results
Homogeneous Ore Domain
Mutual inductance versus relative magnetic permeability for homogeneous ore domain.
Sense coil current versus time for constant relative magnetic permeability along homogeneous ore domain.
Steady-state window:
–

## Slide 10: Results
Heterogeneous Ore Domain
Increasing cv → stronger local permeability contrasts → lower overall mutual inductance (M).
High cv (more heterogeneous texture) → magnetite becomes more dispersed → weaker magnetic coupling.
The effect of heterogeneity diminishes when < 4, where differences in M are less pronounced.
Grain size () for cv = 1 has negligible influence on M
Mutual inductance versus relative magnetic permeability for different levels of across heterogeneous ore domain.
Mutual inductance versus relative magnetic permeability for different levels of cv across heterogeneous ore domain.

## Slide 11: Concluding remarks
Magnetic-based monitoring was explored as an alternative to density-based systems for ore-grade estimation in magnetite-rich iron ore.
The current LHD density-based system is limited by fragmentation, loading-volume variation, and moisture content.
The proposed magnetic concept shows promising results for both ore–waste differentiation and ore-grade estimation, sensitive to variations in magnetic permeability.
Mutual inductance (M) serves as a robust metric to track effective low-field permeability and thus ore grade.
Future work should assess:
  Influence of water content, natural joints, and mineral veins on the response.
    Conductivity effects (moisture) are expected to be less significant in magneto-quasi-static DC regime.
  Non-linear B–H characterization of specific Kiirunavaara ore types.
  Validation against drill-core grades and field calibration across different fragment positions and levels.
Notes: These steps will enable calibration coefficients and support integration into real-time LHD monitoring systems.