## Slide 1
This project has received funding from the European Union’s Horizon 2020 Framework Programme for research and innovation under grant agreement No 768701.
More info on www.sharkproject.eu
Femto-second laser texturing prediction using COMSOL Multiphysics®
E.C. Chevallier¹, V. Bruyère¹, G. Bernard² and P. Namy¹
¹: SIMTEC, Grenoble, France
²: GFMS, Meyrin, Switzerland
Developing laser surface texturing from the current trial-and-error, lab-scale concept to a highly predictable, data driven industrial approach.
FEMTO-SECOND LASER TEXTURING:
Laser surface texturing (LST) is a non-contact process that shows excellent repeatability as well as the ability to achieve small-size features.
The use of ultra-short laser pulses in LST offers the possibility to reduce significantly the amount of molten material hence increase the quality of the finishing.
Model prediction possibilities:
It is possible to make predictions on the shape of a single and multi-impact craters.
Further work on the model would include the development and experimental validation of the prediction of the topography produced after hundreds of ultra-short laser impacts.
Keep this space clear for COMSOL use. Remove this text box before submitting.
Figure 1: Energy transmission phases of the femto-second laser source to the lattice.
FEMTO-SECOND LASER ABLATION MODELLING:
Thermal problem: the Two-Temperature Model
Continuous model used to describe the time evolution of the temperatures of the sub-systems by coupled differential equations:
Where is the temperature of the system, subscripts and denotes the electrons and the lattice respectively. and are the specific heat capacity, mass density and thermal conductivity. is the electron-phonon coupling constant and is the laser source term.
Laser ablation modelling
Numerical convective heat flux
Where is a numerical parameter and is the vaporization temperature.
Vaporization modelling using deformed geometry with the mesh velocity set at the liquid/gas interface :
Where is the surface normal vector and is the latent heat of vaporization.
Figure 2: Electron and lattice temperature evolution during the laser impact of 100 fs.
Figure 3: Multi-impact crater progression using fs laser ablation.
Temperature (K)
Time (s)
Phase 1
Phase 2