## Slide 1: Numerical Simulation of the Time-Dependent Permeation Through Barrier Structures
Dr. Oliver Miesbauer
Jing Tang
Chair of Food Packaging Technology
Technical University of Munich

## Slide 2
Source: Fraunhofer IVV
permeance
Barrier performance of polymer films of thickness 100 m
Barrier requirements of technical products
permeance

## Slide 3
  Inorganic-polymeric multilayer structures
  Deposition of metals or transparent oxides, nitrides from gas phase
  Deposition of polymers from gas or liquid phase
Concepts of barrier structures
  Polymeric layers with dispersed particles
  Inorganic particles: sheet silicates, graphene
  Shape of particles: platelets, fibers
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschichtstrukturen, Dissertation, 2017

## Slide 4
Models for barrier structures
  Polymer: permeable phase  Fick‘s diffusion equation
  Inorganic layers and particles: impermeable phase
  Transport through circular defects of inorganic layers  Dirichlet boundary condition
  Oriented, cuboid shaped particles
  Zero normal flux condition at polymer / inorganic interfaces
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschichtstrukturen, Dissertation, 2017

## Slide 5
Finite element simulation
Tetrahedral mesh for permeable inorganic layer on top of polymeric substrate
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschichtstrukturen, Dissertation, 2017
  COMSOL Multiphysics: numerical solution of the transient diffusion equation for the model structures in 2 or 3 dimensions
  General Form PDE
  Tetrahedral mesh
  Comparison with analytical results  FEM results are reliable even for thin layers.

## Slide 6
3-dim. steady-state permeation through inorganic layer / polymeric layer / inorganic layer
norm. defect distance
0
10
norm. polymer thickness
norm. flux
  Defects of the inorganic layers are decoupled, if polymeric intermediate layer is sufficiently thick  Elongation of the diffusion path length (tortuous path).
  Numerical simulation: Decreasing the thickness of the polymeric intermediate layer reduces permeance, if the layer is sufficiently thin.
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschicht-strukturen, Dissertation, 2017

## Slide 7
3-dim. transient permeation through inorganic layer / polymeric layer / inorganic layer
Polymer
Inorganic
Inorganic
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschichtstrukturen, Dissertation, 2017

## Slide 8
3-dim. transient permeation through inorganic layer / polymeric layer / inorganic layer
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschichtstrukturen, Dissertation, 2017
Polymer
Inorganic
Inorganic
  Flux from polymer through defect into gas phase: time required for approach to steady-state increases with polymer thickness and defect distance.
  Quasi-steady-state approach (Q.s.): Mass balance for polymer layer
Polymer thickness << defect diameter

## Slide 9
2-dim. steady-state permeation through a polymeric layer with dispersed nanoparticles
  Permeable channels between impermeable particles
  Concentration profile in channels is nearly 1-dimensional and linear.

## Slide 10
2-dim. transient permeation through a polymeric layer with dispersed nanoparticles
  Reducing the volume fraction of permeable matrix or increasing the aspect ratio of the particles  decrease of permeance and extension of time required to reach steady-state
  1-dim. concentration profile  Lag time is nearly proportional to (diffusion path length)2.
  Volume fraction of permeable matrix
  Layer without particles
  Aspect ratio of particles
  Layer without particles

## Slide 11
Thank you for your attention
Dr. Oliver Miesbauer, Chair of Food Packaging Technology, Technical University of Munich
Phone: +49.8161.71.3595, Email: oliver.miesbauer@tum.de