## Slide 1: Light Enhancement and Direction Control Using Bowtie Antenna Arrays
Isabel Pita, Ning Liu, and Brian Corbett

## Slide 2: Presentation Outline
Bowtie Antenna Applications and Array Potential
Bowtie Antenna Array Design in COMSOL
Methods for Optical mode measurement
Gaussian Beam Design
Propagation along Substrate
Comparison to Single Antenna
Conclusions and Applications

## Slide 3: Uses of Bowtie Antenna
Enhanced Surface Plasmon Propagation
Z. Fang et al, Nano Lett., 11, 1676, 2011
M. Kaniber et al, Sci. Rep., 6, 23203, 2016
Strong and Confined Near Field Enhancement
High Scattering Resonance Between Tips

## Slide 4: Antenna Array Geometry
Gold Antenna
Air-Glass Interface
260 nm
740 nm
X
Y
X
Z

## Slide 5: Geometry Featuring Gold Strips
Lens Configuration
Gold Trench Addition
X
Y
X
Z

## Slide 6: Gaussian Beam Shaping

## Slide 7: Change in Direction With Wavelength
E
E
1150 nm
650 nm
Higher Wavelength Changes Direction
High
Low

## Slide 8: Propagation with Change in Polarization
E
E
In both the optical mode propagates perpendicular
Better Control of Surface Plasmons
High
Low

## Slide 9: Measured Mode Propagation
 | Antenna ratio 3 ↑↑↑/1↑ | 
Polarization | 0⁰ | 90⁰
↔ | 3.51 | 1.41
↕ | 2.15 | 8.50
 | Antenna ratio 3 ↑↑↑/1↔ | 
Polarization | 0⁰ | 90⁰
↔ | 0.15 | 2.12
↕ | 1.78 | 2.54

## Slide 10: Propagation With Gold Trenches
E
Strong SPP Direction Control
E
1 Au Antenna
3 x Au Antenna
High
Low

## Slide 11: Propagation With Gold Trenches
E
Strong SPP Direction Control
E
3 x Au Antenna
1 Au Antenna
High
Low

## Slide 12: Trench Cut Enhancement (100 nm)
 | Antenna ratio 3 ↑↑↑/1↑ | 
Polarization | 0⁰ | 90⁰
↔ | 0.04 | 0.22
↕ | 3.60 | 8.07
 | Antenna ratio 4 ↑↑↑↑/1↑ | 
Polarization | 0⁰ | 90⁰
↔ | 0.01 | 0.76
↕ | 4.93 | 15.06

## Slide 13
Arrays of bowtie antennas allow for direction control at higher wavelengths
Allow improved SPP control
Provides better enhancement than a single bowtie antenna
Potential uses in nano-optics devices
Nano-dot excitation
Switch behaviour
Conclusions and Applications
If a picture needs a caption it can look like this.

## Slide 14
Dr. Ning Liu and Dr. Brian Corbett.
III-V Materials and Devices Group, Photonics Centre, Tyndall National Institute
Nanophotonics and Nanoplasmonics Group, Department of Physics, University of Limerick.
This work was funded by the Irish Research Council Postdoctoral Fellowship Fund GOIPD/2018/10

## Slide 15
Tyndall National Institute,
Lee Maltings,
Dyke Parade,
Cork,
Ireland.
T12 R5CP
t: +353 21 490 4177
e: info@tyndall.ie
tyndall.ie