## Slide 1: Simulation of bi-material nano-second laser ablation
M. DALa, L. CARVALHOb, A. SEMEROKb, W. PACQUENTINb, H. MASKROTb
a PIMM-ENSAM umr CNRS 8006
b Den – Service d’Etudes Analytiques et de Réactivité des Surfaces (SEARS)

## Slide 2: Outline
Introduction
Physical Models
Results and validation
Analysis
Conclusion & complementary works

## Slide 3: Introduction
Wavelenght: 1064 nm Gaussian beam
Beam size (1/e²) : 62 µm Impulsion duration : 110 ns
Frequence : 20 kHz Peak power : 104 W
Topic :
Nanosecond laser ablation for nuclear decontamination
Context :
Experiment: cea
Simulation: PIMM
Simulation aims to:
Understand current mecanism(s)
  Phase explosion
  Solid cracking
  Vaporization
Parameters | Min | Max
Laser fluence | 5 J/cm² | 12 J/cm²
Shots overlaping | 60 % | 90 %
Nb treatement | 1 | 10
Laser
Head
Diagnistics
Sample

## Slide 4: Introduction
GDMS (1 track, 73 J/cm²)
Satisfactory results but it still few cantaminant
Treat residual contamination
Understand mechanism to improve process
Optimisation des paramètres de décontamination
Paramètre | Min | Max
Fluence laser | 5 J/cm² | 12 J/cm²
Recouvrement spatial | 60 % | 90 %
Nombre de balayage | 1 | 10
Echantillon brut
Echantillon oxydé
Echantillon décontaminé
Decontaminaion efficientcy
Before decontamination
After decontamination

## Slide 5: Physical models
Principle
Simulated geometry
Heat transfers
Fluid flows
Free boundaries
Chemical species transport

## Slide 6: Physical models
Heat transfers

## Slide 7: Physical models
Fluid flow
Free boundary (ALE - hyperelastic)
Ablation velocity
Conservative
in mass
Not conservative
(material withdrawal)

## Slide 8: Physical models
Chemical species
Mass lost  ALE
Numerical aspects
Linear interpolations
Fully coupled problem
700 000 elements  2 500 000 DOF
Nearly 8 hours to be solved

## Slide 9: Results and validation
Residual Eu: 0.28 % Model vs 0.2 % Experiment
Ablated mass 3,3 mg vs 5,5 mg numerically
Reasons:
Shots overlap in experiment (not in simulation)
Material properties …
Experiment radius
Simulation radius
Radius (µm)
Laser Fluence (J/cm2)

## Slide 10: Analysis
Remarks :
Oxide melts before metal
Oxide evaporates before metal
Oxide thermics is faster than metal
Oxide vaporization larger
Assumptions:
Phase explosion
Solid fracturation
Oxide vaporization

## Slide 11: Conclusion & complementary works
Ablation model (to improve)
Satisfactory results compared to experiments
This case is probably driven by vaporization - > increase the power
More [thèse L. Carvalho]
Mono impact without oxide
Heat transfers 3D
Complex geometries (noches)

## Slide 12: Conclusion
Perspectives
Vapour simulation ?
Material properties (Tvap, Lvap, …)

## Slide 13: Annexes

## Slide 14: Annexes

## Slide 15: Results and validation
Solid phase only
Full model
Analytical model**
COMSOL model
Analytical model**
COMSOL model
Temperature (K)
Temperature (K)
Error (%)
Error (%)
Time (µs)
Time (µs)