## Slide 1: Thermal Analysis of DED process and COMSOL feasibility in Mechanical Modeling of AM process
Vaibhav Nain*1, Muriel Carin2, Thierry Engel3, Didier Boisselier1, Christophe Cordier3
1 IREPA LASER, Parc d’Innovation, 67400 Illkirch, France
2 Univ. Bretagne Sud, UMR CNRS 6027, IRDL, F-56100 Lorient, France
3 Institut National des Sciences Appliquées, 67000 Strasbourg, France
Grenoble, 14-15 Oct 2020

## Slide 2: Directed Energy Deposition (DED)
Powder DED (P-DED): Process Principle
DED System
  Co-axial nozzle with focused laser and a stream of powder, both intersecting at a common focal point generally in an inert environment
Process Physics
  The energy density generated at a particular point leads to the melt pool formation and incoming powder is fed in the melt-pool leading to the formation of a bead
DED Advantages
  Fabrication of large parts possible
  Minimum powder wastage
Figure 1: DED process schematic [1]
Figure 2: DED part fabrication
(Height: 500mm; Ø: 600 mm)
[1] X. Guan and Y. F. Zhao, “Modeling of the laser powder–based directed energy deposition process for additive manufacturing: a review,” Int J Adv Manuf Technol, vol. 107, no. 5, pp. 1959–1982, Mar. 2020, doi: 10.1007/s00170-020-05027-0.

## Slide 3: Why model P-DED process ?
Distortion & Residual Stresses
DED Process
  Due to the complex thermal cycles in DED process, it leads to the generation & accumulation of unwanted levels of distortion & residual stresses
DED Disadvantages
  Unwanted levels of distortion & residual stresses
  Leads to crack formations, misalignment & failure of parts
DED Process still not understood due to
  It involves complex multiple heat cycles
  Lack of understanding of accumulation of distortion & residual stress
  Complicated evolution of microstructure of build materials
Modeling can help to
  Develop the better understanding of process physics
  Predict & minimize deformation & residual stresses
  Achieve the objective FABRICATE PART FIRST TIME RIGHT
(a) Crack
(b) Mismatch
Figure 4: DED fabricated part failure due to crack generation & misalignment during & after deposition
Figure 3: Large Scale DED fabricated part & Distortion accumulation leading to rejection of part (Fabricated part length: 1100mm)
(a) Fabrication
(b) Distortion

## Slide 4: Numerical Model
Development of the model for P-DED
Thermal Model
Equivalent Heat Source
Numerical Material Deposition
Heat Losses
Material Properties f(T)
Input
Mechanical Model
Transient Thermal
Model Results
Accurate transient 3D Thermal Model is a pre-requisite to develop Thermo-Mechanical model for P-DED.
So, in the present work a transient 3D Thermal Model is developed in COMSOL Multiphysics® 5.5.

## Slide 5: Thermal Model for P-DED
Use of COMSOL Multiphysics® 5.5
Use of COMSOL for Thermal Model for DED

## Slide 6: Thermal Model for P-DED
Numerical Model Development
Figure 5: Intensity Distribution
Goldak Double Ellipsoid Source
Equivalent Numerical Heat Source
Numerical Material Addition/Deposition
  Quiet/Active Element Activation
  Quiet Elements: Weak Thermal Properties
  Active Elements: Temperature dependent Thermal properties (Metal)
  Activation Criterion:
Heat Equation
Heat Losses
Activated Elements
Quiet Elements
Active
Elements
Moving Heat Source
Static Mesh
Figure 6: Schematic of Quiet/Active Element Activation method
PROCESS PHYSICS
NUMERICAL MODEL
LASER
POWDER SPRAY
CONDUCTION
BUILD PART AND SUBSTRATE
HEAT LOSS
MELTING
MELT POOL & SOLIDIFICATION
Dynamics
Heat transfer

## Slide 7: Thermal Model for P-DED
Experiment results (from literature [2])
Experiment Set-Up
Process Parameters
Deposition Pattern
Thermocouple Location & Measurement
Process Parameter | Value
Feedstock Type | 
Substrate & Feedstock Material | Stainless Steel 316L
Mass feed rate | 7.5 g/min
Dimensions | 
Substrate | 100×30×8 mm3
Deposited Layer | 65×1.2×0.6 mm3
Number of Layers | 30
Mass feed rate | 7.5 g/min
Laser Parameters | 
Laser Power | 400 Watt
Laser Scan Speed | 600 mm/min
Laser Spot Radius | 0,6 mm
Figure 8: Thermocouple location [2]
[2] M. Biegler, B. Graf, and M. Rethmeier, “In-situ distortions in LMD additive manufacturing walls can be measured with digital image correlation and predicted using numerical simulations,” Additive Manufacturing, vol. 20, pp. 101–110, Mar. 2018, doi: 10.1016/j.addma.2017.12.007.
Table 1: Process parameters [2,3]
[3] M. Biegler, A. Marko, B. Graf, and M. Rethmeier, “Finite element analysis of in-situ distortion and bulging for an arbitrarily curved additive manufacturing directed energy deposition geometry,” Additive Manufacturing, vol. 24, pp. 264–272, Dec. 2018, doi: 10.1016/j.addma.2018.10.006.
Substrate
Figure 7: Zig-Zag Deposition Pattern
Patterned Layers

## Slide 8: Thermal Model for P-DED
Numerical Model Set-Up
Model Definition
CAD Design
Material Properties
Mesh Strategy
Substrate
Pattern Layers (20)
New Layers (10)
Figure 9: CAD design done in Comsol Design Module
(a) Original Mesh
(b) Single Refinement
(c) Double Refinement
Figure 11: Original Mesh & Mesh Refinement along the width of track
Figure 10: Temperature dependent Material Properties [2]
(a) Thermal Properties [2]
Chart: Temperature (°C)
| 20 | 200 | 400 | 600 | 800 | 1000 | 1100 | 1200 | 1380 | 1500
Conductivity | 14 | 16 | 19 | 21 | 23 | 26 | 28 | 30 | 32 | 32
Density | 7900 | 7850 | 7800 | 7750 | 7710 | 7660 | 7610 | 7560 | 7430 | 7200
(b) Mechanical Properties [2]
Chart: Temperature (°C)
| 20 | 200 | 400 | 600 | 800 | 1000 | 1100 | 1200 | 1380 | 1500
Specific Heat | 472 | 488 | 505 | 527 | 562 | 628 | 698 | 719 | 740 | 750
Young's Modulus | 198 | 187 | 172 | 157 | 141 | 106 | 10 | 5 | 2 | 2

## Slide 9: Thermal Model for P-DED
Numerical Model Implementation
Model features
Material Addition
Heat Transfer Analysis
Mesh Strategy
COMSOL modules used
Design Module
Heat Transfer in solids
  Heat Source
  Heat flux (convective heat flux)
  Surface-to-ambient radiation
Structural Mechanics
  Linear Elastic Material
    Activation
Figure 12: Quiet/Active method material activation
(c) Layer 10 Deposition
(a) Layer 1 Deposition
(b) Layer 2 Deposition
(d) Deposition process finishes
Activation Criteria COMSOL:

## Slide 10: Thermal Model for P-DED
Model features
Material Addition
Heat Transfer Analysis
Mesh Strategy
(a) Heat Transfer analysis during Layer 1 Deposition
(b) Heat Transfer analysis during Layer 2 Deposition
(c) Heat Transfer analysis during Layer 10 Deposition
(d) Fabrication process finishes
Figure 13: Heat Transfer Analysis during P-DED process
Numerical Model Implementation
COMSOL modules used
Design Module
Heat Transfer in solids
  Heat Source
  Heat flux (convective heat flux)
  Surface-to-ambient radiation
Structural Mechanics
  Linear Elastic Material
    Activation

## Slide 11: Thermal Model for P-DED
Numerical Model Implementation
Figure 14: Temperature evolution at TC 1 and TC 2 with different mesh refinement
(a) TC 1
(b) TC 2
(a) No refinement
(b) Single refinement
(c) Double refinement
Figure 15: Effect of Mesh Refinement on Accuracy of Heat Transfer (Layer 1 deposition)
Model features
Material Addition
Heat Transfer Analysis
Mesh Analysis
Mesh Type | No. of elements | Dof (solved for) | Computation time
Original Mesh | 9602 | 73440 | 1 hour
Single Refinement | 14340 | 97920 | 1 hour 56 min
Double Refinement | 19078 | 122400 | 2 hour 35 min

## Slide 12: Thermal Model for P-DED
Numerical Model Validation
Temperature Results
Process Simulation
Comparison b/w experimental & numerical results
Figure 16: Comparison b/w Experimental & Numerical results
Animation 1: P-DED Thermal Model process simulation
Numerical model shows good agreement with experimentally measured trends of temperature evolution during the process

## Slide 13: Mechanical Model for Additive Manufacturing (AM)
COMSOL Feasibility Test
SATOH Test: Software benchmarking (Complex Thermo-Mechanical behaviour)
Advantage of SATOH: To represent AM process heating & cooling cycle and validate material properties & mechanical behaviour law
Figure 17: Conditions of Mechanical constraints & temperature cycle of SATOH test
[4] L. Depradeux, “Simulation numérique du soudage - Acier 316L : validation sur cas tests de complexité croissante,” These de doctorat, Lyon, INSA, 2004.
[5] G. Tran Van, “Détermination d’un critère de fissuration à chaud par liquation en fonction de la teneur en bore et de sa localisation pour l’acier inoxydable austénitique 316L.,” These de doctorat, Lorient, 2018.
Chart: Axial Stress Curve-SATOH Temperature test
Figure 18: Comparison of experiment results with numerical results obtained with different software
COMSOL modules used
Design Module
Heat Transfer in solids
  Temperature
Structural Mechanics
  Linear Elastic Material
    Viscoplasticity
Multiphysics
EVP: Elasto Viscoplasticity Model

## Slide 14: Mechanical Model for Additive Manufacturing (AM)
COMSOL Feasibility Test
SATOH Test: Software benchmarking (Complex Thermo-Mechanical behaviour)
Figure 19: Conditions of temperature loading & unloading cycle [4]
Chart: Comparison of Stresses obtained with different Material Properties & Hardening Law
Cycle 2 (888°C) | 287.293 | 274.033 | 245.304 | 207.735 | 148.066 | 88.3978 | 35.3591 | -15.4696 | -57.4586 | -99.4475 | -137.017 | -163.536 | -185.635 | -196.685 | -196.685 | -194.475 | -196.685 | -190.055 | -190.055 | -185.635 | -190.055 | -181.215 | -181.215 | -167.956 | -148.066 | -141.436 | -137.017 | -86.1878 | -41.989 | 8.8398 | 59.6685 | 72.9282 | 92.8177 | 112.707 | 125.967 | 130.387 | 141.436 | 154.696 | 167.956 | 174.586 | 181.215 | 192.265 | 203.315 | 220.994 | 232.044 | 236.464 | 254.144 | 276.243 | 304.972 | 318.232
Cycle 3 (663°C) | 309.392 | 282.873 | 229.834 | 130.387 | 30.9392 | -57.4586 | -114.917 | -165.746 | -194.475 | -203.315 | -203.315 | -207.735 | -212.155 | -139.227 | -103.867 | -103.867 | -88.3978 | -64.0884 | -13.2597 | 41.989 | 61.8785 | 72.9282 | 121.547 | 145.856 | 159.116 | 176.796 | 185.635 | 198.895 | 218.785 | 225.414 | 243.094 | 260.773 | 298.343 | 320.442
Cycle 4(461°C) | 327.072 | 260.773 | 163.536 | 55.2486 | -26.5193 | -92.8177 | -143.646 | -179.006 | -205.525 | -212.155 | -214.365 | -181.215 | -161.326 | -112.707 | -57.4586 | -6.6298 | 50.8287 | 81.768 | 103.867 | 123.757 | 154.696 | 198.895 | 227.624 | 243.094 | 269.613 | 293.923 | 309.392 | 331.492
Figure 20: Comparison of experiment results with numerical results obtained from COMSL with different material model & hardening laws
COMSOL modules used
Design Module
Heat Transfer in solids
  Temperature
Structural Mechanics
  Linear Elastic Material
    Viscoplasticity
    Elastoplasticity
Multiphysics
COMSOL Multiphysics demonstrates its feasibility in modeling Additive Manufacturing (AM) process by predicting the stress behaviour due to complex heating and cooling cycle (same type of cycle in AM) with different material plasticity laws & material properties
EVP: Elasto Viscoplasticity Model
EP: Elastoplasticity Model

## Slide 15: Future Work
Development of Thermo-Mechanical Model for P-DED
  Transient Thermal Model validation for different material
    Ti-6Al-4V
    Inconel 718
    Inconel 625
  Development of Quasi-Static Mechanical Model
    Comparison of Numerical results obtained with different material hardening laws
    Validation of Mechanical Model with experiment results

## Slide 16: Contact: vn@irepa-laser.com
Thankyou