## Slide 1
Numerical simulation to improve the -barrier property of films by integration of water absorbers
M.Sc. Jing Tang
Dr. Oliver Miesbauer

## Slide 2: Barrier requirements of technical products
permeance
Barrier performance of polymer films of thickness 100 m
Source: Fraunhofer IVV

## Slide 3: Permeation through polymer/nano-particle composites
  Effects of impermeable particles dispersed in a permeable matrix
    Reduction of free volume for dissolution and diffusion of molecules, reduction of diffusion cross-section area
    Hindrance to diffusion  tortuous and therefore extended diffusion paths

## Slide 4: Models for barrier structures
  Polymer: permeable phase  Fick‘s diffusion equation
  Particles: impermeable phase
  Transport through polymeric matrix
  Oriented, cuboid shaped particles
  Zero normal flux condition at polymer / inorganic interfaces
Oliver Miesbauer, Analytische und numerische Berechnungen zur Barrierewirkung von Mehrschichtstrukturen, Dissertation, 2017

## Slide 5: Difference between the Modeling of barrier composites against and
  - barrier film
  Impermeable particles dispersed in a permeable matrix
  Concentration is a continuous function of time and place
  - barrier film
  Permeable water absorbers dispersed in a permeable matrix
  Concentration is not a continuous function of place at the interfaces between two permeable phases

## Slide 6: Modeling of polymer/water absorber composite
; (fick‘s laws)
Theoretical basis
Simple model for the water vapour transport (diffusion and sorption) in the layer ( or and
(henry‘s law)
linear isotherm

## Slide 7: Finite element simulation
  COMSOL Multiphysics: numerical solution of the transient diffusion and sorption equations for the model structures in 2 or 3 dimensions
  General Form PDE
  Physics-controlled mesh
  Comparison with analytical results  FEM results are reliable even for thin layers.
Example: physics-controlled mesh for polymeric layer with water absorbers

## Slide 8
3-dimensional model
transparent geometries for two different matrices with 10 rows of uniform dispersed, permeable and spherical particles with a relative radius
Two different polymer matrices with particles
M1: matrix with shifted particles
(b) M2: matrix with unshifted particles
Dimensionless: described by relative length
Thickness:
Relative Thickness: to .
Relative radius:
Relative solubility coefficient:
Relative diffusion coefficient:

## Slide 9
Comparison of results of two different matrices
Influence of solubility coefficient:
Comparison diagram for M1 and M2 with particles with different solubility coefficients but same size.
Stationary permeation & time to appoach the stationary status: with particles > no particles.
The saturated permeation & time lag ↑ with the increasing of.
No big difference between two matrices

## Slide 10
Influence of size of particles:
Comparison diagram for M1 and M2 of particles with same solubility coefficient but different sizes.
8.72
3.52
Comparison of results of two different matrices
Stationary permeation ↑ with the increasing relative particle radius
Time lag ↑ with the increasing
No big difference but: stationary permeation of M2 of particles with is almost 2.5 times that of M1

## Slide 11
Influence of diffusion coefficient of particles
Comparison diagram for the two arrangements of particles with different diffusion coefficients
The stationary permeation ↑ with the increasing
time to approach the state of stationary permeation ↓ with increasing particle diffusion coefficient.
Permeability for M1: 2x of M2
Time lag for M1: longer than M2
Comparison of results of two different matrices

## Slide 12
Other influencing factors
Particle row number
Number of particles at a fixed filling degree
Shapes of the particles…
Aspect ratio of particles
Volume fraction of polymer matrix
Spatial distribution of particles
Orientation: rotation of particles
Important influencing factors for - barrier films
for -barrier film

## Slide 13
Thank you for your attention
M.Sc. Jing Tang
Chair of brewing and beverage technology
TUM School of Life Sciences
Technical University of Munich
Tel: +49 8161 71 4379
Email: jing1.tang@tum.de