## Slide 1: Numerical study of effective thermal conductivity (ETC) of periodic complex structures to be used in concentric distillation column
COMSOL Conference 2020 Europe (14 & 15 October 2020)
By: Yousef Al-Maqaleh (PhD student at INP Toulouse)
Supervisors: David Rouzineau (INP Toulouse)
Michel Meyer (INP Toulouse)
Nathalie Raimondi (Paul Sabatier University)

## Slide 2: Outline
Objective of the study
Studied geometries
Model
  Computational domain
  Boundary conditions
  Calculation of effective thermal conductivity (ETC)
Results
  Mesh convergence study
  Domain size sensitivity study
  ETC versus porosity
Conclusion

## Slide 3: Objective of the study
The goal of this study : heat transfer by conduction performance only
  Evaluate the effective thermal conductivity (ETC) in W/m/K of different geometries
  Discriminate the best geometry based on their ETC
    Good indicator of thermal performance
    Calculate a correlation of ETC wrt porosity
Radial Heat flux
Internal wall
Rectifying zone
Stripping zone
Stripping zone
Liquid flow
Gas flow

## Slide 4: Studied geometries
Tetra-Spline (TS) Lattice geometry Patented (tested on normal distillation column)
  Mass transfer ✓
  capacity ✓
  heat transfer ?
Internal wall
TS packing bloc design with a consolidated internal wall for concentric column
(Photo from Autodesk Inventor)
TS elementary unit design
Photo from Autodesk Inventor

## Slide 5: Model : computational domain
Specifics about TS geometry
  perfectly periodic horizontally (x and y)
  not periodic vertically (in z direction)
Important parameters of TS geometry
  The porosity (ϵ) varies with:
    Strand diameter ds (mm) – variable
    Strand length l1=l2 (mm) – variable
    Angles of both tetrahedrons θ1 =30° and θ2 =40°
  (m3)
    n=1:6
  *EU=elementary unit
n=1 n=2 n=3

## Slide 6: Model: boundary conditions
Solved equation : energy balance
    at phase interface
Used physics in COMSOL : Heat transfer in Solids and Fluids
Two zones:
  Fluid= air (fixed properties, stagnant)
  Solid= Aluminum (fixed properties)
Boundary conditions
  Hot surface: T =70°C
  Cold surface: T=68°C
ETC calculated according to:
  x direction
  y direction
  z direction (irrelevant for concentric column)
Boundary condition placement for 1 EU domain
ETCx ETCy ETCz
Fixed Physical property | Al | Air
Thermal conductivity – λ (W/(K.m)) | 238 | 0.0295
Heat capacity – Cp (J/(kg.K)) | 900 | 1008.5
Density – ρ (kg/m3) | 2700 | 1.025

## Slide 7: Model: Calculation of ETC
Calculation of the heat flux
  Volume-averaged heat flux in the direction perpendicular to the Temperature BCs
    Ex: heat flux in the x direction
  Surface-averaged normal heat flux to the Temperature BCs
    Calculated in hot or cold BC
Calculation of effective thermal conductivity ETC:
  in second method (Randrianalisoa, et al., 2015)
  * Approximation only valid for small ΔT
Or
Either

## Slide 8: Results: mesh convergence study
Mesh convergence study done on one TS geometry with:
  ds=2.25mm _ l1=l2=15.35mm _ ϵ=89%,
  Domain n=1 EU*
Results: between the coarse mesh and extremely fine mesh, there is only 0.75% relative deviation for ETCx
  The model converge easily with a coarse mesh, chosen mesh: 15 nodes/mm3
  Modification was made to refine packing meshing (by modifying minimum element size)
Model is insensible to the relative tolerance value set in the study :
  Relative tolerance used=1e-3 (by default)
Chart: Number of nodes per domain volume (nodes/mm3)
| 2.1924758995188873 | 3.7478598587498602 | 7.8113590498627099 | 16.510876995006512 | 29.009566253060513 | 58.955324324732075
Mesh, Element size min≠max | 3.9257 | 3.9464 | 3.9492 | 3.9571 | 3.9582 | 3.9553
Coarse | Optimal | Extremely fine
2 Nodes/mm3 | 15 Nodes/mm3 | 59 Nodes/mm3
56149 Tetrahedrons | 375792 Tetrahedrons | 1534790 Tetrahedrons
*EU=elementary unit

## Slide 9: Results: Domain size sensitivity study
The domain size was changed from 13 to 63 EU* for TS geometries with different parameters:
  Naming code: TS-material_ds_l1=l2_ϵ_SpecificArea direction of ETC (x or y)
Results: no need to simulate a TS domain size larger than 23 EU
Note: Calculation time varied from 2 minutes to 2 hours depending on the domain size
Chart: n, Domain volume =n*EU_volume
| 1 | 2 | 3 | 4 | 5 | 6
TS_Al_2.25_89_182 x | 4.8584 | 4.5935 | 4.5579 | 4.5316 | 4.5196 | 4.5113
TS_Al_1.5_92_205 x | 3.343 | 3.161 | 3.1384 | 3.1196 | 3.111 | 3.1048
TS_Al_2,75_89_148 x | 4.7151 | 4.4559 | 4.4559 | 4.3959 | 4.3845 | 4.3759
TS_Al_2.00_87_231 x | 5.9774 | 5.665 | 5.6296 | 5.5996 | 5.5855 | 5.5748
TS_Al_2.25_89_182 y | 4.4232 | 4.5571 | 4.5644 | 4.5812 | 4.578 | 4.5859
TS_Al_1.5_92_205 y | 2.9942 | 3.1252 | 3.1321 | 3.1477 | 3.1477 | 3.1539
TS_Al_2.75_89_148 y | 4.2813 | 4.4177 | 4.4177 | 4.4427 | 4.4404 | 4.4483
TS_Al_2.00_87_231 y | 5.5036 | 5.6313 | 5.6449 | 5.6627 | 5.6558 | 5.665
TS_Al_2.25_89_182 Avg | 4.6408 | 4.5753 | 4.5611 | 4.5564 | 4.5488 | 4.5486
TS_Al_1.5_92_205 Avg | 3.1686 | 3.1431 | 3.1353 | 3.1336 | 3.1293 | 3.1294
TS_Al_2.75_89_148 Avg | 4.4982 | 4.4368 | 4.4368 | 4.4193 | 4.4124 | 4.4121
TS_Al_2.00_87_231 Avg | 5.7405 | 5.6481 | 5.6373 | 5.6312 | 5.6206 | 5.6199
n=1 n=2 n=3
Horizontal heat flux
Surface: Temperature (°C)
*EU=elementary unit

## Slide 10: Results : ETC versus porosity
ETC horizontal (x and y avg) versus porosity >0.85% for TS geometry
Results: TS geometry is not efficient in horizontal (radial) heat transfer by conduction
Note:
  ETCx,y (TS_2.25_15.35_89) = 4.8 W/(m.K)
  ETCz (TS_2.25_15.35_89) =18.5 W/(m.K) orientation of the geometry is vital
Vertical Heat flux
Horizontal heat flux
Surface: Temperature (°C)
Chart: Porosity (%)
| 0.87123428613905962 | 0.89006273377692957 | 0.89254703126232593 | 0.91784749569831026
EFC_x,y avg_TS Simulation ((W/(m.K)) | 5.6199 | 4.5486 | 4.4121 | 3.1294
EFC_x,y TS correlation ((W/(m.K)) | 6.7846 | 6.4757 | 5.5741 | 4.5485 | 4.4168 | 3.1294
EFC_z_TS Simulation ((W/(m.K)) | 21.859 | 18.5475 | 13.5869

## Slide 11: Conclusions
Estimations of ETC for TS geometries was achieved with reliable numerical results using COMSOL Multiphysics
The geometry was imported to COMSOL Multiphysics from Autodesk Inventor using CAD Module
ETC is dependent on :
  Geometry
  Orientation of the geometry (same as the heat flux or opposite)
  Porosity
  Intrinsic conductivity of the material
In concentric distillation column: heat transfer is radial (horizontal)
  TS is not very conductive in the horizontal direction
  TS vertical conductivity is high but not relevant to the application
A correlation for TS horizontal ETC is obtained as:
(Calmidi & Mahajan, 1999)
  * a=0.181 and b=0.763, is porosity, and are fluid and solid conductivities resp.

## Slide 12: Thank you for your attention

## Slide 13: References
Calmidi, V. V. & Mahajan, R. L., 1999. The effective thermal conductivity of high porosity fibrous metal foams. Journal of Heat Transfer, 121(2), pp. 466-471
Randrianalisoa, J., Baillis, D., Martin, C. L. & Dendievel, R., 2015. Microstructure effects on thermal conductivity of open-cell foams generated from the Laguerre-Voronoï tessellation method. International Journal of Thermal Sciences, 17 8, Volume 98, pp. 277-286
Photos were taken from
  Autodesk Inventor ® 2020
  COMSOL Multiphysics ® 5.5