## Slide 1
Modelling of microstructure parameters in a high temperature and pressure alkaline electrolysis cell
Matteo Lualdi
Morten Siwertsen

## Slide 2: Who we are
We are a team of dedicated, experienced and enthusiastic experts within Multiphysical simulation, Data Analysis & Machine Learning.
We have strong backgrounds within Chemical & Process Eng., Physics and Mechanical Engineering
Contacts:
info@resolvent.dk
www.resolvent.dk

## Slide 3: Outline
Introduction
  Eeehy project
  Importance of the study
Modeling approach
Results
Conclusion and next steps

## Slide 4: Introduction - EEEHY project
EEEHy: Economic and Efficient Electrolytic Hydrogen production

## Slide 5: Importance of the study
Why is microstructure modeling and optimization important?
  What is the maximum achievable performance
  What is the effect of a specific parameter on the performance
  What direction should the development take
Notes: High temperature and high-pressure alkaline electrolysis is a new technology with low TRL so even electrocatalyst and cell morphology design is need to be outlined almost from scratch so the use of simulation can basically guide development answering questions like: maximum achievable performance, quantify the effect of parameters, guide the direction of the development

## Slide 6: Introduction – physics
Alkaline electrolytic cell
Electronic transport
Charge transfer reaction (Butler-Volmer)
Ionic transport (migration and diffusion)
Diffusion of the dissolved gas
Bubble nucleation and growth
Bubble release and transport to macropores
Gas diffusion in macropores network
Mesoporous matrix with liquid electrolyte
Cathode: HER
2H2O+2e-↔2OH-+H2
Anode: OER
4OH- ↔ 4e-+O2 +H2O
I
I
OH-

## Slide 7: Modelling approach-simplifying assumptions
Anode: OER
4OH- ↔ 4e-+O2 +H2O
I
Mesoporous matrix with liquid electrolyte
OH-
Half-cell steady-state model in 2D
Electronic transport
Charge transfer reaction (Butler-Volmer)
Ionic transport (migration and diffusion)
Diffusion of the dissolved gas
Bubble nucleation and growth -> nucleation potential
Bubble release and transport to macropores
Gas diffusion in macropores network
Start as simple as possible
Notes: Green is taken fully care of
Balck is check with nucleation potential

## Slide 8: Introduction – physics and length scales
Mesoporous matrix with liquid electrolyte
Cathode: HER
2H2O+2e-↔2OH-+H2
Anode: OER
4OH- ↔ 4e-+O2 +H2O
I
I
OH-
10-100 μm
Dmacropores:1-10 μm
~500μm
1-10 μm
Dmesopores:25-50 nm

## Slide 9: Modeling approach-simplifying assumptions
I
I
10-100 μm
Dmacropores:1-10 μm
1-10 μm
Dmesopores:25-50 nm
Mesoporosity is
homogenized (ξ, τ, av)
Mesoporous matrix with liquid electrolyte
Cathode: HER
2H2O+2e-↔2OH-+H2
Anode: OER
4OH- ↔ 4e-+O2 +H2O
I
I
OH-
~500μm

## Slide 10: Modeling approach-porous electrode geometry 2D
Random microstructure geometry based on 3 controlling parameters:
  Agglomerate size (D)
  Electrode thickness
  Number of spheres (Aimed porosity)
D=10 μm
thickness=100 μm
Aimed porosity 30%
Effective por=25%
D=5 μm
thickness=50 μm
Aimed porosity 30%
Effective por=20%
D=2.5 μm
thickness=100 μm
Aimed porosity=30%
Effective por=20%

## Slide 11: OER – effect of the electrode thickness
Effect of electrode thickness
D=2.5 μm
T=150 °C, P= 30 bar, 1 A/cm2, pH2O = 1.7 bar
σ=100 S/cm
Overpotential decreases when increasing electrode thickness from 20 to 100 μm of ~10%
thickness=20 μm
thickness =50 μm
thickness =100 μm

## Slide 12: Moving to 3D
Random spheres creates a meshing nightmare

## Slide 13: Moving to 3D
Presence of electrode structure taken care at “material level”
“scale” factor (we scale the material properties)

## Slide 14: 3D Modelling approach
Body fitted mesh
Easier to mesh
Non-body fitted mesh
Difficult to create a meaningful mesh for spheres with random contact points

## Slide 15: OER –effect of the electrode thickness
Effect of electrode thickness
D=2.5 μm
σ=100 S/cm
Operating conditions :T=150 °C, P= 30 bar, 1 A/cm2, CKOH= 45 wt%, pH2O = 1.7 bar
Thickness=10 μm
Thickness=20 μm
Thickness=50 μm
Notes: Just few word about the porosity, here we aimed at porosity 35 and the porosity of for set 1 and 2 points were 0.31-0.33. For set 3 it was a bit high, 43%

## Slide 16: OER –effect of the electrode thickness and operating conditions
Effect of electrode thickness
D=2.5 μm
σ=100 S/cm
Chart: Electric Potential at current collector
| 10 | 20 | 50
Set1 | 179.7772 | 150.3251 | 117.4878
Set 2 | 169.3148 | 142.4386 | 113.7818
Set 3 | 110.4259 | 82.6168 | 52.0417
Operating conditions
Set1:T=150 °C, P= 30 bar, 1 A/cm2, CKOH= 45 wt%, pH2O = 1.7 bar
Set2:T=200 °C, P= 30 bar, 2 A/cm2, CKOH= 45 wt%, pH2O = 6 bar
Set3:T=200 °C, P= 30 bar, 0.5 A/cm2, CKOH= 45 wt%, pH2O = 6 bar
Notes: Just few word about the porosity, here we aimed at porosity 35 and the porosity of for set 1 and 2 points were 0.31-0.33. For set 3 it was a bit high, 43%

## Slide 17: OER –effect of agglomerate diameter
Effect of agglomerate size
Erod_thick=20 μm
σ=100 S/cm
Chart: Bubble formation potential
| 2.5 | 5 | 1
Set1 | 3.8868 | 6.1437 | 1.2983
Set 2 | 9.5044 | 4.5669 | 1.4783
Set 3 | 1.106 | 1.7267 | 2.8604
CO2/CO2sat ~300 for bubble nucleation

## Slide 18: Conclusion and next steps
Thick electrode (>50μm) would be beneficial
Bubble formation not risk for the agglomerate diameters of interest
Quantification of effect of operating conditions
Validate model against experimental results

## Slide 19
Thank you for your attention