## Slide 1
COMPUTATIONAL METHODS: Similar to Plasmonic Wire Grating application. The aim of our calculation is to obtain electric field vector E for all (x, y, z) by solving the wave equation.
Boundary conditions
[AC], [CE], [EG], [BD], [DF] and [FH]:
[AB]: out-of-plane E = (0, 0, 1) and in plane H = (0, 0, 1) periodic incident wave
Automatic diffraction order reflectance calculation
First step: Comparison between the DE ex-situ measurement and the analytic DE calculation using the Bessel functions of the first kind and m-th order [1]
and results modeled in COMSOL 5.5. using Wave optics module.
Incident
wave
Diffracted wave
RESULTS: Spatial distribution of the electric field and dependence of the reflectance (order 0, -1 and 1) on
the grating depth for three
different angle of incidence.
Variable | Value | Units
Grating period d | 860 | nm
Wavelength  | 532 and 635 | nm
As20Se80 thickness [EC] | 970 | nm
Angle of incidence  | 0, 5 and 10 | deg
Grating depth h | from 0 to 150 | nm
CONCLUSIONS: Dependence on incident wave orientation increase
with grating depth. Overall quite good agreement between results
from COMSOL, calculation with the Bessel functions and the measurement allows the utilization of measurement of diffraction efficiency as a tool to estimate depth of the grating.
Open questions: Accuracy of the experiment?
Influence of non-zero transmittance for red diode?
Cause of difference in case of green LED?
REFERENCES:
P. Hariharan, "Optical Holography: principles, techniques, and applications," Cambridge Studies in Modern Optics, second Edition, p. 47 (1996).
Figure 3. Diffraction grating simulated geometry
Table 2. input parameters of the model
Figure 4. Optical properties of As20Se80 layer obtained from ellipsometry
Figure 1. Schematic diagram of hot-embossing
diffraction grating fabrication process
Diffraction Efficiency of Gratings with Sinusoidal Profile
P. Janicek1,*, V. Stepankova1, M. Kurka1, K. Palka1, A. Ventura2, J. G. Hayashi2
1. Faculty of Chemical Technology, University of Pardubice, Pardubice, 53210, Czech Republic
2. Optoelectronics Research Centre, University of Southampton, Southampton, SO17 1BJ, UK
*e-mail: petr.Janicek@upce.cz
Excerpt from the Proceedings of the 2020 COMSOL Conference in Grenoble
Wavelength (nm) | 532 | 635
Refractive index (substrate) | 1.5168 | 1.5132
INTRODUCTION: Investigation of the diffraction efficiency (DE) measurement as a tool to fabricate a diffraction grating with a defined thickness.
[AB] = d
[CD] parametric curve
Figure 6. Comparison of measured and calculated DE for
a) green LED b) red LED
ACKNOWLEDGEMENT: Authors appreciate financial support from grant LM2018103 from the Ministry of Education, Youth and Sports of the Czech Republic and European Regional Development Fund-Project “High-sensitive and low-density materials based on polymeric nanocomposites – NANOMAT” ( CZ.02.1.01/0.0/0.0/17_048/0007376).
Table 1. input parameters of the model
Figure 5. Spatial distribution of electric field
norm for h = 100 nm,  = 10 deg
 = 635 nm
in-plane
 = 532 nm out-of-plane
Figure 2. Custom-made equipment
for the diffraction efficiency measurement