## Slide 1: Coupled A-H Field Formulation For HTS Magnets In COMSOL Multiphysics ®
L. Bortot1,2, I. Cortes Garcia1, H. De Gersem1, M. Mentink2, J. Van Nugteren2, S. Schöps1, A. Verweij2
Special Thanks: B. Auchmann (PSI), F. Grilli (KIT), M. Maciejewski (CERN)
14-15 October 2020, Online Event

## Slide 2: INTRODUCTION
High temperature superconductors (HTS)
Copper oxides (CuO2)
Doping with La, Bi-Sr-Ca, Y-Ga-Ba etc.
Higher critical temperature and coercive field with respect to low-temperature superconductors (LTS)
Quench
Local transition from superconducting to normal conducting state
In high energy-density applications (e.g. accelerator magnets), potentially irreversible effects!
Mitigation: artificial resistive zone increase  dilution of the Ohmic loss density
■ Copper ■ ReBCO ■ Substrate
Resistive zone
HTS tape
Figure: schematics of a copper-coated ReBCO tape

## Slide 3: FORMULATION (EXCERPT FROM POSTER)
Magnet domain decomposition
active region  Coils:
superconductors (
normal conductors
passive region  Iron yoke, air region:
normal conductors
insulators (
Field equations [1]
 |  | formulation in
 |  | formulation in
 |  | Heat balance equation in
 |  | Current constraint
 |  | Voltage distribution function
 |  | Current constraint
 |  | Voltage distribution function
Figure: General representation of the computational domain
[1] Bortot, L., et al. "A Coupled A–H Formulation for Magneto-Thermal Transients in High-Temperature Superconducting Magnets." IEEE Transactions on Applied Superconductivity 30.5 (2020): 1-11.

## Slide 4: DISCRETE EQUATIONS
Discretization functions
Edge elements for , ( 1st and 2nd order)
Nodal elements for , (1st order)
Circuit interface
External circuit connected via electric ports
FEM model  one-port component with impedance
form | Weak form PDE module
𝐇-form | 
Coupling terms | 
Heat Balance | Heat transfer in solids
Circuit coupling | Global ODEs and DAEs
 | Weak form PDE module
𝐇-form | 
Coupling terms | 
Heat Balance | Heat transfer in solids
Circuit coupling | Global ODEs and DAEs

## Slide 5: NUMERICAL EXAMPLE
HTS solenoid protected by heater strips: 2D axisymmetric model and circuitry
2D FEM model
Iron core
Holder
Coil
Insulation
Heater strips
Figure: Rendering of the HTS solenoid. Part of the insulation is removed for illustration purposes.
A.
B.
Coil supply loop
Heaters supply loop
0
t (ms)
5
10
150
Protection mode
A. crowbar resistance
B. Heater strips
Current discharged

## Slide 6: NUMERICAL RESULTS (1/2)
Circuital currents
Peak temperature
Chart: time (ms)
Chart: time (ms)
Chart: Quench detection time (ms)
| 0 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 18 | 20
T | 168.2222 | 182.8245 | 198.5568 | 215.5101 | 233.7835 | 253.4302 | 274.6589 | 297.6125 | 322.4305 | 349.3411 | 378.5494
 | 300 | 300
Max. detection time
Figure: Current decay in the coil (left) and current discharge in the heater strips (right)
Figure: Adiabatic hotspot temperature in the coil, as a function of the quench detection time
Induced quench
Heater strips

## Slide 7: NUMERICAL RESULTS (2/2)
100 ms
150 ms
50 ms
20 ms
30 ms
10 ms
Temperature distribution in the superconducting coil, as a function of time
Temperature (K)
Quench
Heat diffusion
Heater strips

## Slide 8: CONCLUSIONS AND OUTLOOK
Figure: Ohmic loss distribution in a HTS solenoid
Figure: magnetic flux density in the Feather-M2 insert dipole magnet
Figure: normalized induced current in a HTS bulk
Conclusions
formulation for HTS applications
Flexibility thanks to the Weak form PDE module
Circuit coupling via the ODEs module
Outlook
Minimization of the quench detection time
Protection of HTS magnets in case of a quench
Dynamics of HTS magnets in accelerator circuits
Thank you for your attention! Contact: lorenzo.bortot@cern.ch