## Slide 1: Time domain simulation of insulating dielectric materials with non-instantaneous polarization
Tianbo ZHOU1, Pierre BIDAN1, Lionel LAUDEBAT1,2, Marie-Laure LOCATELLI1
1 - LAPLACE, CNRS, INPT, UPS, Toulouse University, France
2 – Institut National Universitaire Champollion, Albi, France

## Slide 2: Sommaire
Introduction
Debye model in time domain
The model in COMSOL
Simulation examples
Conclusions

## Slide 3: Introduction Theory of polarization
Kao K 2004 Dielectric Phenomena in Solids: with Emphasis on Physical Concepts of Electronic Processes (San Diego, CA: Elsevier)
The dielectric medium is polarized under the influence of the applied field E
The polarization cannot response instantly to an applied field.
Polarizations can be divided into instantaneous polarization and non-instantaneous polarization
Debye model traits the dipolar polarization
Polarization types of normal dielectric materials under a step­ function electric field (1)
Debye model

## Slide 4: Introduction Problem background in COMSOL
A critical factor (overvoltage/overcurrent) for the design of electric insulating devices appears in transient state
COMSOL | Instantaneous polarization | Non-instantaneous polarization
Frequency domain | Yes | Yes
Time domain | Yes | No
Steady state | Transient state
Yes | No
Yes | Yes
A method based on time domain simulation and integrating the Debye model equations in COMSOL is proposed
The situation in transient state in consideration of the dielectric relaxation (non-instantaneous polarization)
System under different types of signal

## Slide 5: Debye model in time domain
The polarization vector evolves in the dielectric material under a step electric field :
(1)
constant time
the instantaneous polarization
the static polarization
Application of electric field
time
Dipole polarization
Dynamic polarization for a step of E
The electric displacement could also be obtained:
(2)
instantaneous permittivity
static permittivity

## Slide 6: Debye model in time domain
(2)
In the invariant and linear case, we obtain following equations under any excitation :
Equivalent electric circuit model
(3)
(4)
The influence of the resistance of material can be introduced by coupling with general Ohm’s law
(5)
is the electric conductivity

## Slide 7: The model in COMSOL
The parallel-plane capacitor description in COMSOL
Property |  |  | 
Value | 1*10-12 | 9 | 3
Property |  |  | 
Value | 1*10-12 | 9 | 3
Simulation parameters for the relaxation dielectric medium
*Time constant will be specified for each simulation case
air
Dielectric medium
electrodes
Integration in COMSOL

## Slide 8: Simulation examples Steady state for a sinusoidal current excitation compared with frequency domain results
Simulation in time domain using the proposed method and simulation in frequency domain
Electric field vs Time in time domain
The distribution of electric field of simulation in frequency domain
The same electric field magnitude in steady state of 2 calculations (about 1.19kV/mm)
Conclusion
  Same results
    Only the steady state in frequency domain calculation
    Steady state + transient state in time domain calculation by using our method

## Slide 9: Simulation examples Transient state results for step and sinus current excitation
Excitation of 5Hz and 50Hz
The Debye model describes the processes of variety of the time dependent polarization from to
Electric field vs Time under step response
Electric field vs Time under sinus (50Hz) response
Electric field vs Time under sinus (5Hz) response
Dielectric relaxation has more influence on the amplitude
in the same order of magnitude
The transient period of Debye polarization appears

## Slide 10
Conclusions
A solution for the simulation in time domain considering the non-instantaneous polarization (dielectric relaxation)
Applied for all types of excitation
Examples demonstrated in a basic geometry under different excitations
Other models such as Cole-Cole, Cole-Davidson or Havriliak-Negami can be integrated in the future