## Slide 2
2
Non-linear Analysis
of
Shroud expansion
Ganesh Bhoye, Dr. Sunita Mohapatra, Ishant Jain
Raychem Innovation Centre,
Raychem RPG Pvt. Ltd., Halol, Gujarat-389350

## Slide 3
3
Shroud for Cable Gland
Shroud give additional ingress protection to cable gland assembly.
Existing Shroud is made up of PVC which have limited elasticity which prohibit the expansion and variability.
New shroud is made up of the Fire retardant and Halogen free material.
Need for FEA Analysis
To select Optimised elasticity for Shroud based on material composition.
To Reduce Tooling cost and tooling Time.

## Slide 4
4
To determine expansion of shroud design using Hyper-elastic Material Module.
For Verification and optimization of the design.
To incorporate modularity in the design.
To optimize thickness of the Shroud for effective material utilization
Optimization (Curve fitting)
  Error Estimation-total squared error
  Model selection
  Material constants estimation
  Input of material constants to the actual geometry
Solid Mechanics (Hyper-elastic simulation)
  Application of the boundary conditions
  Meshing
  Analyze and postprocessing
  Results
Physical Phenomenon:
  Sliding expansion
  Direct expansion
Fig. Sectional View of the shroud design
Problem Definition

## Slide 5
5
Optimization study for Curve fitting
Material behavior to be predicted.
Curve fitted to stress strain curve data from UTM after processing.
Following material models were used,
  Arruda Boyce
  Yeoh
  Mooney Rivlin 9- parameter,
  MR-5 Parameter,
  MR-3 Parameter
  MR-2 Parameter
  Ogden 6 and 8 parameter model
Total squared error-
  Model with least squared error is selected.
  best fit model is used i.e. Mooney Rivlin 9 parameter model fits best for this data.
Determination of parameters i.e. Material constants like C01, C10, C11, C12, C02, C20, C21, C03, C30.
Uniaxial tensile testing data
Biaxial tensile testing data
  Mooney Rivlin 9 parameter model fits best for selected material composition.

## Slide 6
6
Curve fitting for uniaxial testing data
Curve fitting for uniaxial testing data
Curve fitting for Biaxial testing data
Curve fitting for Biaxial testing data
Optimization study for Curve fitting
  More realistic material behavior can be predicted from Biaxial Tensile test Data

## Slide 7: FEA –Hyper-Elastic Study
Expansion Phenomenon- Boundary conditions and Meshing
Direct Expansion
Sliding expansion
7
Fixed Constraint
Prescribed displacement
Contact
Sliding Expansion
Mesh Generation
Contact
Prescribed displacement
Fixed Constraint
Direct Expansion
  Expansion with two types have been determined to find maximum deformations and critical points in design and to optimize thickness.

## Slide 8
8
FEA –Hyper-Elastic Study
Direct Expansion
  Maximum Expansion and critical points can be observed in this type of expansion.

## Slide 9: FEA –Hyper-Elastic Study
9
Sliding expansion
  Sliding Expansion is more practical approach similar installation of shroud

## Slide 10
Concluding Remarks
  Though Sliding Expansion is more practical approach, Maximum radial expansion can be observed in Direct expansion variant.
  It was clear from the results that minimum expansion of 7.5 mm can be achieved failure (tearing of shroud) i.e Shroud can be expanded by 15 mm diametrically.
  Hence single size of the shroud can be used for more than 3 Cable glands.
  Effect of thickness of the shroud has also been determined and optimum thickness has been selected for product.
  Application of Optimization and Hyper-elastic module in Design phase of the product can reduce tooling cost and tooling time significantly.

## Slide 11
THANK YOU
11

## Slide 12
12
Meshing

## Slide 13: FEA –Hyper-Elastic Study
Expansion Phenomenon
Direct Expansion
Sliding expansion
13