## Slide 1: FEM modeling of highly strained monocrystalline ZnTe/CdTe core-shell hetero-nanowires
Serhii Kryvyi, Slawomir Kret, Dorota Janaszko, Jakub Plachta, Piotr Wojnar
Institute of Physics, Polish Academy of Sciences, al. Lotnikow 32/46, 02-668 Warsaw, Poland
COMSOL Conference 2020 Europe
October 14–15

## Slide 2
Motivation
Extremely high surface to volume ratio
Ability to obtain defect-free structures even on highly mismatched and “exotic” substrates
Axial hetero-NW
Radial hetero-NW
Two types of hetero-nanowires:
Applications:
Various sensing applications
Nanoscale optoelectronics and photonics
Micro- and Nano-Electro-Mechanical Systems
Transistors ...
SEM image of ZnTe nanowires on Si substrate
Material 1
Material 2
Material 1
Material 2
The core-shell configuration introduce complex anisotropic 3D lattice distortion comparing to 2D tetragonal distortion of epilayers on thick substrate.
10 - 100nm

## Slide 3
Au
Alloy
Si (111)
Alloy
Alloy
Te
Zn
Te
Zn
Te
Zn
Si (111)
Si (111)
Te
Cd
Te
Cd
Core-shell nanowires
CdTe shell
ZnTe core
Hetero-nanowires fabrication
1
2
1 - 4μm
Diameter: 20 - 100nm
ZnTe
Molecular Beam Epitaxy:
Vapor-Liquid-Solid mechanism
Sample
Effusion cells
MBE
T ~ 380°C
T ~ 340°C

## Slide 4
Receiving TEM data
e-beam
60 px
50nm
Scanning Nanobeam Electron Diffraction
24 px
b)
a)
FEI Titan Cubed 80-300
Probe size
Diffraction pattern
High Angle Annular Dark Field image of NW
High resolution TEM image part of NW
Lattice constant:
aZnTe = 6.103Å
aCdTe = 6.483Å
zinc blende structure

## Slide 5
Strain in axial (grown) direction - εzz
Strain in radial direction - εxx
In-plane tilt
(deg)
Strain mapping
Experimental diffraction pattern
Relative strain:
=
d – interplanar spacing
g - reciprocal lattice vector

## Slide 6
α=0°, β=1.2°
α=1.2°, β=0°
α=0°, β=0°
Experimental diffraction pattern
Simulated stack
Local orientation mapping

Cross-
correlation
Nanowire
Local orientation maps
α - tilt
β - tilt
6

## Slide 7
FEM modeling of core-shell hetero-nanowires
Solid Mechanics
Linear Elastic
Initial Stress and Strain
7
ZnTe:
Anisotropic elastic material
CdTe:
[111]
[1-10]
[11-2]
Crystallographic directions
Model
Simulation
240 nm
von Mises stress

## Slide 8
Relative strain in axial direction - εzz
In-plane tilt
(deg)
α – misorientation
(deg)
Comparison FEM simulation and experiment results
Simulation
Experiment
Simulation
Experiment
Simulation
Experiment

## Slide 9
Conclusions
Proposed approach for strain and orientation mapping for single nanoobject with nanometer resolution which is not achieved even for a synchrotron!
Obtained good agreement FEM simulation and experimental data
Further works:
Taking into account Nonlinear Elastic Strain in model
Expand the model for simulation piezoelectric and magnetostriction effects
The research was supported by National Science Centre (Poland) by grant: UMO-2016/21/B/ST5/03411

## Slide 10
Thank You for attention