## Slide 1
An approach to verify the water transport model in organic coatings
E. Jalilian1, M. Meeusen2, B. Wouters2, G. Van Assche1, A. Hubin2, H. Terryn2
1Vrije Universiteit Brussel (VUB), Research Group Physical Chemistry and Polymer Science, Pleinlaan 2, B-1050 Brussels, Belgium
2Vrije Universiteit Brussel (VUB), Research Group Electrochemical and Surface Engineering, Pleinlaan 2, B-1050 Brussels, Belgium
Notes: Kop
10/2/2020
Voet
1

## Slide 2
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 2
INTRODUCTION
GoalS
Advanced Materials industry
  Extend service life
  Sustainable material concepts
  Higher performance (multifunctionality)
Lifetime and ageing testing of coatings
  Formulation stage (initial product formulation + testing) months
  Application stage (optimization application parameters) months
  Internal testing months
  Accelerated testing (standards ISO, NORSK,…) 6/9 months
  Field testing (long-term testing) 3/5 years+
  Total = 4-10 years (application)
CURRENT Approach (STATE OF THE ART)

## Slide 3
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 3
AIM: Develop an integrated corrosion modelling tool that is reliable and predictive (20-30 years)
  Integrated: subsystems (metal/coating/electrolyte) + phenomena (transport/interfacial (electro)chemistry/delamination) in 1 model
  Combined experimental & modelling (FEM) approach
  Experimental: mechanistic insight + input parameters model + validation model
INTRODUCTION
APPROACH
Model
INPUT
OUTPUT & VALIDATION
PARAMETER OPTIMIZATION
FTIR
EIS
1
2
3

## Slide 4
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 4
AIM: Develop an integrated corrosion modelling tool that is reliable and predictive (20-30 years)
  Integrated: subsystems (metal/coating/electrolyte) + phenomena (transport/interfacial (electro)chemistry/delamination) in 1 model
  Combined experimental & modelling (FEM) approach
  Experimental: mechanistic insight + input parameters model + validation model
INTRODUCTION
APPROACH
Model
INPUT
OUTPUT & VALIDATION
PARAMETER OPTIMIZATION
FTIR
EIS
1
2
3
Rel Cf & Cb afo time (hours/days)
@ coating/substrate interface

## Slide 5
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 5
2. MODEL
Model
INPUT
Gravimetry
FTIR
EIS
1
2
3
OUTPUT & VALIDATION
PARAMETER OPTIMIZATION
1D model
Time-dependent water transport through coating
  Diffusion
    D diffusion constant
  Adsorption/Desorption reaction
    Cf concentration free water
    Cb concentration bound water
    kads adsorption rate
    kdes desorption rate
    Θf_max max fraction of sites for free water
    Θb max max fraction of sites for bound water
INPUT
VARIABLES
MODEL PARAMETERS
1D
[mol/m³] !!!

## Slide 6
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 6
2. MODEL
Model
INPUT
Gravimetry
FTIR
EIS
1
2
3
OUTPUT & VALIDATION
PARAMETER OPTIMIZATION
Necessary to define initial values & boundary conditions
    Adsorption/desorption reaction
      Reaction rate
      Boundary conditions (B.C)
        Chemical equilibrium @ H2O/coating interface
          obtained by R=0 and substituting
    Initial Values
    No flux condition
1D
No Flux
B.C.

## Slide 7
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 7
3. OUTPUT & VERIFICATION
OUTPUT
Model
INPUT
Gravimetry
FTIR
EIS
1
2
3
PARAMETER OPTIMIZATION
OUTPUT & VALIDATION
Cf vs d afo time
Cb vs d afo time
Time
Time

## Slide 8
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 8
3. OUTPUT & VERIFICATION
OUTPUT - POSTPROCESSING
Model
INPUT
Gravimetry
FTIR
EIS
1
2
3
PARAMETER OPTIMIZATION
OUTPUT & VALIDATION
Concentrations c permittivities ε
capacitances C
virtual impedance plots Z

## Slide 9
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 9
SUMMARY & CONCLUSIONS
Model
INPUT
OUTPUT & VERIFICATION
PARAMETER OPTIMIZATION
1
2
3
FYSC:
Coating thickness (d)
Chemistry (MM, ρ)
Gravimetry:
  D
  Max water uptake
Conc,free f(time, d)
& Conc,bound f(time, d)
SURF:
(ORP-)EIS Bode plot
  C
  Ɛ
  D
  Water uptake
SURF:
ATR-FTIR Kretchmann
(coating/metal)
  Rel. Conc free
  Rel. Conc bound
Conc Ɛ
C
Bode plot
kads – kdes – θsat – θbound_sat
Diffusion
Adsorption/Desorption
…
EC (Corrosion)
Delamination
Blue: modelling
Green: verification exp. parameters
Red: verification modelling results
Now

## Slide 10
M. Meeusen – An approach to verify the water transport model in organic coatings
10/2/2020 | 10
THANK YOU !!!
QUESTIONS ?