## Slide 1: An interaction between electromagnetic field and materials:
Characterization of mechanical stress in ferromagnetic materials using Eddy current non-destructive techniques
Safae Bouterfas, PhD student, EOBE, Univ. Paris-Saclay
Laurent Daniel, University Professor, CentraleSupélec
Yann Le Bihan, University Professor, Univ. Paris-Saclay
Laurent Santandréa, Engineer, CNRS

## Slide 2: Plan
Context
Eddy Currents Non-Destructive Testing
Model definition
Finite Element Method: COMSOL
External Function
Results
COMSOL CONFERENCE 2020 EUROPE

## Slide 3: Context
COMSOL CONFERENCE 2020 EUROPE
Txx
Txx
Tyy
Tyy
eL
eR
eΘ
3D stress in gas pipelines
Local 2D stress
Villari effect
Ferromagnetic material
[Dahia et al. 2015]

## Slide 4: Eddy Currents Non-Destructive Testing
COMSOL CONFERENCE 2020 EUROPE
Hp
I
Hs
JEC
Ferromagnetic specimen
Excitation coil
Evolution of Eddy Currents in depth of a conductor material
Skin depth
Hs(µ(T))  EC sensor: Z(T)
µ(T)
Notes: Eddy currents are created in the extreme surface of the conductor plate when its subjected to a dynamic magnetic field excitation.

## Slide 5: Model definition
COMSOL CONFERENCE 2020 EUROPE
AMSM: Magnetic permeability µ(UH,T)
COMSOL: Magnetic fields H and B
EC sensor impedance Z(T)
Magnetic field direction UH
Stress tensor T
Finite element method

## Slide 6: Finite Element Method: COMSOL Geometry definition
COMSOL CONFERENCE 2020 EUROPE
EC sensor
Pipeline
Study domain
Infinite element domain
Boundary Layers
Mesh
NDT using EC

## Slide 7: Finite Element Method: COMSOL EC sensor impedance
COMSOL CONFERENCE 2020 -EUROPE- October 2020
AC/DC Module: Magnetic and Electrical Fields
Frequency study: from 1 kHz to 1MHz
Z = R + j Lω
PJ = R I²eff
Wmag= ½ L I²eff
Study domain
Specimen

## Slide 8
COMSOL CONFERENCE 2020 EUROPE
Results Magnetic flux density: induced stress anisotropy
Without stress
Under stress: Txx=150MPa

## Slide 9: Model definition
COMSOL CONFERENCE 2020 EUROPE
AMSM: Magnetic permeability µ(UH,T)
COMSOL: Magnetic fields H and B
EC sensor impedance Z(T)
Magnetic field direction UH
Stress tensor T
External function
C code

## Slide 10: External function Multiscale model:
COMSOL CONFERENCE 2020 EUROPE
Magneto-elastic behavioural law of a ferromagnetic material:
Polycrystal
Domaine
Single-crystal (grain)
Material parameters :
Elastic Coefficients
Magnetic Constants
Magneto-elastic Constants
Texture data (SEM measurement)
T
µ (H, T)
Magnetic permeability [H/m]
Mechanical stress [N/m2]
[L. Bernard et al., 2011]

## Slide 11: External function Analytical version of the Multiscale Model:
COMSOL CONFERENCE 2020 EUROPE
x
y
z
Txx
Txx
φ
θ
H
w
v
uH
[Daniel, 2013]
AMSM’s parameters:
Magnetic permeability:
µr(0,T)=1+
H field :
Stress tensor :

## Slide 12: Model definition
COMSOL CONFERENCE 2020 -EUROPE- October 2020
AMSM: Magnetic permeability µ(UH,T)
COMSOL: Magnetic fields H and B
EC sensor impedance Z(T)
Magnetic field direction UH
Stress tensor T
Implementation

## Slide 13: Finite Element Method: COMSOL Implementation of stress effect
COMSOL CONFERENCE 2020 EUROPE
External material:
Example ID: 32321
C code  .dll/.so
Hypothesis:
H & B field colinear in the plan (XY) of the material

## Slide 14: Finite Element Method : Comsol Model algorithm:
COMSOL CONFERENCE 2020 EUROPE
Initial solution « µ(T) » : H
AMSM
µ(H,T)
B(T)
NL Eq system (Newton Raphson)
Direction of B(T)
Impedance signal
External Function

## Slide 15
COMSOL CONFERENCE 2020 EUROPE
Results Magnetic flux density:
Without stress
Under stress: Txx=300MPa
Under stress: Tyy=300MPa

## Slide 16: Conclusion
Implementation of the stress effect on the magnetic properties using a multiscale approach
The model is yet to be improved
COMSOL CONFERENCE 2020 EUROPE
Laurent.santandrea@geeps.centralesupelec.fr
Safae.bouterfas@geeps.centralesupelec.fr
Laurent.daniel@geeps.centralesupelec.fr
Yann.le-bihan@geeps.centralesupelec.fr